Ashes Recyling and Heavy Metals Recovery

# Based on the following reports

[NLAP-PCS 2018] Chapter 8

[NLAP-PCS 2019] Chapter 6,7,8,9

Trainee Report Concept for Automation for Ashes Reycling Test Rig (6 July 2020)

# Heavy Metals Recycling: Overview

# Ashes Recycling Unit (From [NLAP-WEDC 2018])

## First Conception Dec 2017

Washing

Solides (Sulfate, …)

## Heavy Metals extraction unit

### COPPER EXTRACTION

Copper extractants for acid leach solutions are exclusively oximes. For extraction from ammoniacal solutions beta diketones may be used. The chemistry of oxime extraction of copper is relatively simple:

Note the following points about this equation:

When M(2+) is extracted two hydrogen atoms are released.

Extraction of 1.0 gpl Cu produces 1.5 gpl H₂SO₄. There are other reactions which take place in copper extraction which can influence extraction and stripping.

#### • Buffering of the aqueous

Dissociation of H₂SO₄:

This dissociation depends on the SO4.

#### Concentration and salts such as aluminium

Sulphate or magnesium sulphate can drive this reaction to the left and reduce the H+ concentration which enhances copper extraction. For this reason highly buffered solutions will yield better copper extraction than non buffered solutions.

#### Dimerisation of the oxime

Oximes can form dimers in the organic phase and this can influence the extraction.

#### Equilibrium Modifiers

These are used in all commercial extractants based on aldoximes and play a most significant role in the extraction of copper influencing not only the equilibrium but also the physical properties of the organic.

#### Extractant Types

Oxime based extractants for copper are largely based on salicyaldoximes which have been modified with one of three modifier types. Examples of the three main extractant types currently in use are:

1. LIX® 984N

A mixture of 2-hydroxy-5-nonylacetophenone oxime and 5-nonylsalicylaldoxime in a

high flash diluent. The acetophenone oxime modifies the aldoxime and also performs as an extractant in its own right.

2. Acorga® M5640

5-Nonylsalicylaldoxime modified with an ester, 2,2,4-Trimethyl-1,3-pentanediol Diisobutyrate (TXIB) in a high flash diluent.

3. LIX® 622N

5-Nonylsalicylaldoxime modified with tridecyl alcohol in a high flash diluent. Each of the extractants marketed by the major chemical suppliers has been designed for a specific type of PLS with regard to pH and copper tenor. Used under the conditions for which they were designed they all deliver very similar copper net transfer values. The physical properties of the various types of extractant do show some differences with the aldoxime/ketoxime mixtures such as LIX984N showing lower entrainments and greater tolerance to crud than the other reagents when treating some types of PLS. The vol% concentration of the commercially available extractants is limited by organic viscosity constraints to about 30-33% and this means that the maximum net transfer of copper will be about 10g/l. For leach solutions containing significantly higher copper tenors than this the throughput O/A ratio will have to be increased above 1.0. Typical copper and acid concentrations for an SX plant treating a dump leach solution of 3.0g/l and pH1.8 are shown in Figure 4.

#### Copper solvent extraction plant configurations

A variety of circuit configurations are used.

• 2E X 1S

The usual circuit for heap leach plants

• 2E X 2S

Used where the copper tenor is above about 7-10 g/l or the PLS pH is less than about 1.2. The decision to use a second strip stage is influenced by the life of the project and the sensitivity of the circuit to the copper tenor of the raffinate. Agitation leach plants for example are sensitive to the loss of copper in a raffinate bleed or in the wash liquor used in the solid liquid separation stages.

• 3E X 2S

These can be justified when the PLS has a very high copper tenor, say above 20- 25g/l and a high 93% plus copper recovery is desired. It is possible to use a 2EX2S circuit under these conditions but the throughput O/A ratios will be high, in excess of 2.5:1 and the capital cost of the 2EX2S plant may be higher than that of the 3EX2S plant. The 3EX2S plant will also be much more flexible in operation.

• 2E X 1W X 1S

The wash stage is used to remove entrained impurities, usually chloride, and entrained and chemically loaded iron.

• 2E X 1P X 1S

Series parallel circuits are used to treat high volumes of low tenor leach solutions. The parallel stage is often retrofitted to maintain copper production when the copper tenor of the PLS falls below project design and there is also the possibility to increase the volume of the PLS flow. Extractant concentrations are higher and copper recoveries are lower in series parallel circuits than in series circuits. Examples of these circuit configurations are shown in Figure 5.

#### Computer modeling of copper extraction circuits

Copper SX circuits have been modeled using a number of techniques. One such model is Henkel’s IsocalcTM TM programme which applies the stability constants for the equilibrium reactions involved in copper extraction to calculate the extraction isotherm for a given leach solution and circuit organic and then applies the McCabe Thiele construction to predict circuit operation. A typical Isocalc print out is shown in Figure 6.

Isocalc can be used in many ways by both project design and plant operating personnel.

• Copper recovery may be predicted for a given PLS, circuit configuration and vol% extractant concentration.

• The reagent inventory cost and copper recovery may be predicted for a variety of circuit configurations.

• A wide range of “what if?” situations may be examined, eg. what if the PLS pH changes from 1.8 to 1.5?

• Operating circuit profiles may be compared with Isocalc predictions. This comparison may indicate the presence of errors in the assumed or measured parameters of the plant, eg. the vol % extractant analysis may be in error.

#### Extractant stability

The oxime based extractants used to recover copper exhibit high chemical stability under normal operating conditions. Chemical attack can take place in the high acid concentrations in strip. Under normal operating temperatures this is not excessive however the degradation rate doubles for every 10oC increase in temperature. At 30oC the half-life of most copper extractants exceeds 150 days and it is only above 50oC that chemical degradation may become an issue. Manganese contamination of the tankhouse may, if the iron level of the tankhouse electrolyte is low, result in permanganate formation and this species can severely degrade both the extractant and the diluent. Bacterial oxidation of the diluent to form carboxylates is relatively common and these ay have a negative effect on the physical and iron transfer characteristics of the organic.

### Nickel extractants

Unlike U/copper extraction where one type of extractant and circuit predominates there is a number of potential nickel extractants and circuit configurations. Sulphide nickel is usually treated using pyrometallurgical routes but in recent years there has been intensive activity in the development of hydrometallurgical routes for both sulphide concentrates and laterites. Nickel deposits can contain valuable quantities of cobalt and copper and these must also be recovered by SX if they are present in sufficient quantity.

Direct solvent extraction of copper, cobalt and nickel from acid leach solutions using oximes, phosphinic acids and versatic acids to extract copper, cobalt and nickel in sequence. While this circuit may function on leach solutions derived from sulphide concentrates, laterite leach solutions contain significant manganese and magnesium, both of which are extracted by phosphinic acid extractants. In addition the aqueous solubility of versatic acid at the pH used for extraction necessitates the inclusion of a versatic acid recovery stage.

### Zinc, cadmium, lead extraction

### SOLVENT EXTRACTION- SOME OPERATIONAL AND EQUIPMENT ISSUES

#### Contactor Design

For the major metals recovered by solvent extraction the mixer-settler contactor design predominates. However there is a range of mixer settler designs available and in recent years there has been some attention refocused on the use of pulsed columns for plants using the kinetically fast ion- exchange extractants. For the chelating extractants which require a minimum of two minutes’ mixer residence time in a well-stirred incinerator, columns have not yet become commercially acceptable. Kvaerner have marketed a variety of the mixer – settler called the combined mixer- settler. As with columns, this unit has only found acceptance for ion-pair extractant systems. Some features of mixer-settlers and columns are given below.

##### Mixer Settlers

• Well established with literally hundreds of operating units.

• Design parameters are well established and very large units treating over 1000 cubic metres per hour of PLS can be designed from bench scale tests.

• Excellent mixing characteristics with control of the optimum droplet size claimed to be possible with modern turbine designs.

• Prediction of capital and operating costs is accurate.

• The phases are readily accessible for sampling and examination in situ.

• Several design varieties are available such as the Bateman Reverse Flow Settler, the Krebs unit and the Outokumpu VSF mixer settler.  The Bateman and Krebs units offer the advantage of installing all of the mixers in a row avoiding the extra piping, walkways and civils involved in the typical head to toe mixer arrangement for conventional mixer settlers. The Outokumpu unit uses a special design of mixer, the vertical smooth flow spiral mixer and pumps the phases from adjacent stages using a dispersion overflow pump. Low power requirements and low entrainments are claimed for the Outokumpu unit.

##### Column Contactors

Advantages claimed for the column contactor include:

• Low area requirements

• Multiple stages within one unit

• Few moving parts

• Low entrainment

• Good vapor conservation

Column installations require piloting for each installation and the flooding conditions for the column must be determined. Recently Olympic Dam Corporation in South Australia has installed a large column plant for uranium extraction. The long residence times in a column compared to a mixer settler can influence the selectivity of the extraction if contaminants have slow extraction kinetics. The main features of conventional mixer – settlers and pulsed columns are shown in Figures 12 and 13.

Figure 56 : OVERVIEW OF KIND OF COLUMNS

Figure 57 :pulsed column

if the fluid in the column and pulse leg are permitted to reach hydraulic equilibrium (valve 2 open), the fluid level will have reached position 1 in the leg with the fluid level maintained at the overflow point in the column. air pressure is now set and the cam started rotating. When v1 is open, v2 is closed which alternately admits and released air into and from the pulse leg. After equilibrium is reached in the system, the fluid in the leg will reach an average position 3 and will oscillate between points 2 and 4. air pressure forces the fluid down from 2 to 4 while the hydraulic head differences between the column overflow and fluid in the leg force the fluid in the leg back from 4 to 2.This interchange of fluid between the pulse leg and column provides the pulse action required in the column .Operating ranges usually encountered in amplitude area from 0.4 to 1.25 inches in the plate section of the column at frequencies from 40 to 100 cycles in minute . the poppet valve and motor are arranged with flange disconnects and electrical plugs-in for ease in replacement of unit needing maintenance. This pulsers are fitted with rotary and liquid sensing devices which close a safety in the event either sensor signals.

Comparison between Bateman column and mixer settler

Bateman column: Flux rates of 30 to 50 m3/m2*h, resulting in very small footprint requirements;

• no evaporation losses or air ingress as the units are sealed;

• improved safety of operation and lower fire risk;

• replacement of several mixer settlers by a single column for the equivalent performance;

• operation in either aqueous- or organic-phase continuity (including the possibility of  dispersing the major phase in the minor phase);

• inclusion of washing or scrubbing operations in the extraction or stripping columns;

• improved phase separation in the settlers, lower entrainment losses, and reduced crud  formation since mixing and mass transfer occur in a very low-shear environment;

• high tolerance of solids or crud in suspension;

• lower maintenance downtime due to few moving parts;

• reduced reagent losses, maintenance costs, and operating costs.

Since columns are particularly appropriate for systems that have rapid kinetics and do not require interstage pH control, the extraction of zinc by di(2-ethyl-hexyl) phosphoric acid (D2EHPA) is ideally suited to this application. The objectives of this study were (i) to determine whether data comparable to the previously optimised results for this system obtained using mixer settlers could be achieved for similar process conditions using a column configuration, and (ii) to validate the claimed advantages of BPCs.

### Freecad design

#### TYPE OF METAL TO CONSTRUCTION

the construction of the column requires a metal that is resistant to corrosion and consequently the destruction. We can have mentioned some metals such as stainless steel that is the best un this case

#### dimension of the extraction column (with rotating discs RDC)

The amount of feed solution that considered as aqueous solution at 90°C (3h) is about 300L(waste +nitric acid ,volume of nitric acid=150 l).

A column of 40 cm radius is suitable in this case.

in most cases found limited to operations where:

• the density differences between the carriers is higher than 50 kg/m³

• the volumetric phase ratio between dispersed drop phase and continuous

phase is in the magnitude of 0.5 < < 5

• the number of theoretical stages NTS  10

Figure 58 : rotating disc contactor

Equilibrium condition on extraction step is in the range of 8-32%extractant volume percent.

| Column | Length (cm) |
| --- | --- |
| Height | 250 |
| Radius | 40 |
| Sheet of stainless steel | 2500×125 |

| Column height / cm | Column active height / cm | Inner column diameter / cm | Inner stator diameter / cm | Outer rotor diameter / cm | Compartment height / cm | Number of compartment in active region |
| --- | --- | --- | --- | --- | --- | --- |
| 150 | 60 | 9.1 | 6.1 | 4.55 | 3.2 | 21 |

Table 28: Characteristics of the RDC column

#### identification of rotor speed

The first and second critical rotor speeds could also be defined based on breakage probability: the first critical rotor speed for a drop with particular size defines as the rotor speed at which the drop breakage starts. In fact, before the first critical rotor speed, the probability of break up for a drop with specific size is zero. Moreover, the second critical rotor speed (for a drop with a particular size) is a rotor speed at which the probability of breaking that drop is equal to 1

The breakage probabilities versus rotor speed for mentioned chemical systems using glassy nozzles with different inner diameters (1.2 and 2.5 mm) to form various drop sizes by adjusting the Qc/Qd ratios and continuous phase heights are presented in next figure regarding to these graphs, the drop breakage increases by increasing the volumetric phase ratio that leads to decrease of the first critical rotor speed. It could be justified with increasing this ratio, the drag forces between the continuous phase and dispersed drops increase results to enhance the probability of drop break up due to collision with the rotors. Mother drop diameter is effective on first critical rotor speed such that the nozzle with larger internal diameter produces larger mother drops with an increase in the probability of break up results to decrement of first critical rotor speed. Increasing the height of continuous phase led to increase of resistance against to upward motion of drops thereupon increment of the break up probability and decrement of the first critical rotor speed. Based on experimental results, the first critical rotor speed for considered chemical system should be 230 rpm.

#### Characteristics of LIX® 984N

Typical properties Physical and performance specifications

| Specific gravity | (25 °/25 °C) 0.935 – 0.955 g/cm³ |
| --- | --- |
| Flash point | Greater than 170 °F=76 °C |
| Copper complex solubility | > 30 g/l Cu at 25 ° |
| Maximum copper loading | ≥ 5.1 g/l Cu |
| Extraction isotherm point | ≥ 4.40 g/l Cu |
| Extraction kinetics | ≥ 95 % (30 seconds) |
| Extraction Cu/Fe selectivity | ≥ 2000 |
| Extraction phase separation | ≤ 70 seconds |
| Strip isotherm point | ≤ 1.8 g/l Cu |
| Net copper transfer | ≥ 2.70 g/l Cu |
| Strip kinetics | ≥ 95 % (30 seconds) |
| Strip phase separation | ≤ 80 seconds |

Table 29: Typical properties physical and performance specifications

| materials | Density (kg/m³) |
| --- | --- |
| Copper | 999 |
| Nitric acid | 1510 |
| Oxime LIX | 806 |

Table 30 :Density of solutions

Figure 59 :input and output of column;

Solvent = light phase (feed at bottom), Solvent = dispersed phase (top interface)

To complete 95% of the extraction process  ,it takes 30 seconds ,in others words of the solute (copper ) passes from solution A(waste + nitric acid ) to solvent . the stripping of copper takes 80 seconds.

| Parts | Dimension |
| --- | --- |
| Covering column | Internal diameter:212 mm Outside diameter:220mm |
| Columns that carry stators | Number:3 Diameter:4 mm Height 2500 mm |
| Stator | Number:10 Internal diameter:120 mm outside diameter:204 mm Height:15 mm Spaced:150 mm |
| Decanter (cylinder+cone) | Number :2 Radius 1:110 mm Radius 2:200 mm Height: 100 mm -Cylinder: Height :300 mm Diameter:400 mm |
| Rotation axis | Diameter :40 mm, height:3500 mm |
| Rotor perforated(20 punch ,D=8 mm ) | Number :10 Internal diameter:40 mm Outside diameter:100 mm Height:15 mm Spaced :150 mm |

Table 31: dimensions of parts of columns

#### Bateman pulsed column

##### Dimensions of Bateman pulsed column

| materials | radius (m) | Height (m) | number |
| --- | --- | --- | --- |
| Stator ring | 0.245 | 0.01 | 19 |
| rotor disk | 0.125 | 0.02 | 19 |
| Main tube | 0.25 | 4 | 1 |
| Tube (driver ) | 0.05 | 8.5 | 1 |
| Inlet & outlet | 0.15 | 0.5 | 2 |

Total surface needed to bateman pulsed column =20.4 m² (11 sheets 1×2 m)

#### Mixer settler

##### Dimensions of Mixer –settler

| Component | Height(m) | Radius (m) |
| --- | --- | --- |
| Mixer 1 | 1 | 0.75 |
| Inlet 1 | 0.2 | 0.1 |
| inlet 2 | 0.2 | 0.1 |
| Outlet 1 | 0.6 | 0.05 |
| Mixer 2 | 1 | 0.75 |
| Inlet 1 | 0.2 | 0.1 |
| inlet 2 | 0.2 | 0.1 |
| Outlet 1 | 0.6 | 0.05 |

| Component | Length (m) | width (m) | Height (m) |
| --- | --- | --- | --- |
| settler | 2 | 0.3 | 1 |
| Barrier to scroll | 2 | 0.3 | 2 |

Total surface needed to mixer=21.2 m²

Total surface needed to settler=6.3  m²

Total surface = 27.45 m² (13 sheet 1m×2 m)

#### RDC column

Figure 60 : overview of RDC column

Figure 61 : top and side face of column

Figure 62 : rotation axis

Figure 63 : rotor perforted (20 perforation, )

Figure 64 : 10 rotor spaced  15 cm

Figure 65 : stator (10 pieces) with rotor

Figure 66 :Distribution of rotors and stators

Figure 67 :Distribution of rotors and stators

Figure 68 :upper and bottom decanter (200 mm of radius, height 300 mm

Cone r1=200mm, height 100 mm)

| parts | Freecad files |
| --- | --- |
| Column |  |
| Rotation axis |  |
| Stator |  |
| rotor |  |
| System |  |

Table 32 :list of parts that formed a system of extraction

#### The Coulumn:

|  | total height: 310 cm |
| --- | --- |
|  | Diameter: 14 cm |
|  | height: 250 cm |
|  | Diameter: 8 cm |
|  | thickness: 2 mm number of disques: 10 |
|  | diameter 1 : 10 cm diameter 2 : 14 cm axe: height: 350 cm |
|  | diameter: 18 cm |
|  | diameter 1 ; 14 cm diameter 2 : 30 cm height: 10 c m |
|  | diameter: 30 cm height : 20 cm |
|  | thickness:2mm |

Manufacturing

# Heavy Metals Recycling Unit (for Cu, Zn, As, Hg, Cd, Cr, Ni, Pb) for 0,8 tons of waste per hour (for 2 MW incineration power plant)

Table of figures

Figure 1: Simple model of TCSR and TSSR	341

Figure 2: TCR	342

Figure 3: Combined series of IPFC	342

Figure 4: Combined shunt series of UPFC	343

Figure 5: Long Rod insulators 3FL	346

Figure 6: Alkaline electrolysis	147

Figure 7:hydrogen generator	148

Figure 8: Three units of 2 MW Enertrag alkaline electrolysis unit - 1000 m3 / h	149

Figure 9: Typical system of an alkaline electrolyzer operating at nearly atmospheric conditions. Purification and gas drying stages are located after low-pressure compression	151

Figure 10: Front and side views of a large alkaline electrolyzer nde-30 with an electrical power of 2 mw (basic design: davy/bamag), operating at (nearly)  atmospheric conditions (Figure courtesy of ENERTRAG HyTec (McPhy).)	151

Figure 11 Monopolar electrolysis	Fehler! Textmarke nicht definiert.

Figure 12:Alkaline Monopolar with tank	Fehler! Textmarke nicht definiert.

Figure 13: Bipolar electrolysis	Fehler! Textmarke nicht definiert.

Figure 14:bipolare	Fehler! Textmarke nicht definiert.

Figure 15: Illustrative cell efficiency and H2 production rate as a function of cell voltage	Fehler! Textmarke nicht definiert.

Figure 16: Reversible voltage as a function of pressure at temperatures T = 25 ,T= 75, and T= 100 in aqueous water electrolysis.	Fehler! Textmarke nicht definiert.

Figure 17: Simulated alkaline electrolyser cell efficiency (HHV) with varying temperature and pressure with a constant current density i = 0.2 A/cm2.  Efficiency is not simulated at points where the prevailing pressure is lower than the vapour pressure of pure water.	Fehler! Textmarke nicht definiert.

Figure 18: Simulated alkaline electrolyser cell efficiency with varying temperature and current density at constant pressure p = 30 bar.	Fehler! Textmarke nicht definiert.

Figure 19: Overview of a typical alkaline electrolysis plant viewed from the hydrogen side. Product (wet) gases from the electrolyser stacks rise to the gas separator tanks where they are separated from the remaining electrolyte. Oxygen gas is treated in its own gas separator tank. Water is continuously added into the system to maintain the desired electrolyte concentration	Fehler! Textmarke nicht definiert.

Figure 20: 10 Overview of exemplary non-pressurized and pressurized water electrolyser systems. Hydrogen buffer storages store hydrogen gas at around 10–30 bar. From the buffer storage, hydrogen gas may be further compressed to 200–700 bar. The highest pressure requirement is in mobility end-use applications, typically 350–800 bar.	Fehler! Textmarke nicht definiert.

Figure 21: System components of Teledyne Energy Systems’ 40 kW alkaline hydrogen generator (Harrison et al. 2009). Measurements of the enclosure are 150 x 178 x 75 cm.	Fehler! Textmarke nicht definiert.

Figure 22: 3 General scheme of a power electronic system	Fehler! Textmarke nicht definiert.

Figure 23: electrolyze PEM	Fehler! Textmarke nicht definiert.

Figure 24: Electrolyser  PEM AREVA H2GEN/CETH2 120 Nm3/h (2015)	Fehler! Textmarke nicht definiert.

Figure 25: The hydrogen chain (documentaire)	166

Figure 26: Schematic of the proposed pre-cooled Linde-Hampson system for hydrogen liquefaction. Ortho-para hydrogen conversion takes place in a HX1 and HX2 zone	171

Figure 27: FreeCad holder of fuel burner	Fehler! Textmarke nicht definiert.

Figure 28: Plant of electrolysis (FreeCAD)	681

Figure 29:Multistack Amperage/Voltage	682

Figure 30: Serial stack	696

Figure 31: Amount of KOH	701

Figure 1: Stepwise experimental procedure adopted for leaching of bottom ash.	802

Figure 2: principle of a separation stage by obtaining a balance	803

Figure 3:ternary diagram	804

Figure 4:Isothermal and isobaric demixing curve.	804

Figure 5:Representation of a ternary system with limited miscibility	805

Figure 6: RDC column (https://kochmodular.com/liquid-liquid-extraction/extraction-column-types/rdc/)	806

Figure 7: heavy metals found in MSWI fly ash (FA) (mg/kg)	806

Figure 8: Heavy metals found in MSWI bottom ash (BA) (mg/kg).	807

Figure 9: Experimental conditions of preliminary leaching tests.	809

Figure 10: Experimental conditions of main leaching test	809

Figure 11:process of separation of copper	811

Figure 12: Flow sheet of the proposed recovery method developed for Cu from fly ash	812

Figure 13:process flow chart	813

Figure 14: . Mass flowscheme of the leaching-extraction process	814

Figure 15: Concentration of metals at each stage: after leaching, in the raffinates after copper and zinc extraction, as well as in the stripping products. nd = not detected.	815

Figure 16: Percentage Extraction of Zn and Fe with 30 vol % Cyanex 272 from bottom ash leachates	815

Figure 17: : Percentage extraction of Zn and Fe with 20 vol % Cyanex 272 from bottom ash leachates	816

Figure 18: Percentage extraction of Zn and Fe with Cyanex 921 from fly ash leachates	816

Figure 6:turbines of 2 MW	Fehler! Textmarke nicht definiert.

In order to built a complete system of heavy metals recovery , we deliver this document  to indicate the process used ,operation,instruments and their cost.

## Introduction

Waste-to-energy is an environmentally sound method for reducing the mass and volume of non-recyclable refuse that would otherwise require landfilling. Combustion typically reduces the volume of the refuse by 90% and reduces the solid mass by 70-80%. The resulting ash, while largely inert, can contain concentrations of heavy metals that require treatment in order to comply with regulations, meet standards for producing a usable product, and to provide for long-term stability of the metals when the ash is exposed in the environment. Heavy metals such as lead and cadmium can be toxic to biological systems when present in high enough concentrations.

The bottom ashes, produced by the industrial incinerators, are an essential secondary raw material resource which has been drawing attention to recover economically important metals.

### Overview of the system of recycling

Fresh bottom ash samples from the burning incineratorswere collected and dried at 25°C. The unburnt parts such as the screw, wire, plastics were separated manually. Prior to leaching tests (discussed in the next section), the sample was reduced to a size of 500 microns with a roll crusher in order to remove the magnetic content (iron removal). the bottom ash samples (tailings and concentrates) were subjected to leaching tests in order to notice the amenability of the samples for metal recovery along with optimization ofnparameters. The step wise experimental procedure adopted is shown in Figure 1 and the following sections details the methodology. It is important to reduced the  size to  500 microns with a roll crusher in order to remove the magnetic contents. the solution is leached and enteres  in a series of  column when the liquid mixes with a suitable liquid extractants to separate the metals from the solution.

Figure 69: Stepwise experimental procedure adopted for leaching of bottom ash.

## Technology of separation

### Principle

Solvent extraction, or liquid-liquid extraction is a separation technique isothermal in a heterogeneous liquid medium.

The method is based on the existence of a difference in the solubility of a substance in two immiscible liquids. The process has three steps, as shown in Figure 1:

- Mixture of the two immiscible liquids, one of them containing the solute,

- Obtaining physico-chemical equilibrium, leading to demixing,

- Separation of the two new liquid phases obtained based on the difference of

densities.

Figure 70: principle of a separation stage by obtaining a balance

Practically, the feed solution F containing solute B dissolved in the diluent A is contacted with the solvent S. The solute B, generally more soluble in the solvent than in the diluent, passes from the solution in the solvent, the solvent enriched in solute is the extract E while the diluent depleted solute is the residue (or raffinate) R.

The passage of solute B from diluent A in solvent S takes place as long as the equilibrium physico-chemical is not reached.

So that the driving force of transfer remains almost constant, the two liquids feeding the column flow against the current.

In order to transport the material as quickly as possible, the area of the transfer surface is increased by various artifices. These objectives can be obtained in a column.

#### The phase equilibrium of ternary mixtures

##### The partition coefficient

A substance B placed in contact with two partially miscible solvents or immiscible S and A is distributed unequally between the two phases that are formed when the physicochemical balance is reached. The ratio of B concentrations in these two phases is the partition coefficient m.

##### The ternary diagram

At equilibrium, these biphasic systems are trivariant. At pressure and temperature constants, they can be represented in a system of triangular axes. The equilateral triangle has the advantage of allowing an equivalent representation for all the constituents. The right triangle has the advantage of being able to expand the scale of one of the axes. It is often interesting to limit the plot to the "useful" part. Each vertex of the triangle represents a pure component. The solute content B, in solvent S and diluent A is expressed in mol%, mass, volume, etc ... and is obtained by a suitable projection on the axis chosen as shown in Figure 3.

Figure 71:ternary diagram

It is easy to demonstrate that the quantity of S and the quantity of the mixture N are in a ratio of the lengths of the MN and MS segments (rule of the lever arm) and that the quantities of two components are in the ratio of projections of the segments on the binary axis corresponding.

Conversely, if the mixture N is added a mass of solvent S, the ternary mixture result is represented by the point M on the line NS such that:

(mass of N)/(mass of S)=MS/MN

##### The demixtion

Figure 72:Isothermal and isobaric demixing curve.

In a ternary system with limited mutual solubility zone (1) stable states,

characterized by a complete miscibility, is separated from the zone (2) unstable states constituting the miscibility gap or diphasic zone, by the solubility isotherm (3) or line "Critical" or demixing curve or equilibrium curve or saturation curve.

Within the miscibility gap, no mixture can exist indefinitely:

any system whose overall composition is represented by point M is divided into two composition phases R and E, points at the intersection of the equilibrium line (4) or conodal RME and the demixing curve f'ff ". At the critical point f the two phases in balance have the same composition.

##### Solvent separation

Figure 73:Representation of a ternary system with limited miscibility

In the zone of total miscibility no separation can take place. However, if starting from an initial mixture F, by the addition of the solvent S, a system whose composition is global M lies within the miscibility gap, which separates into two phases R and E. Phase R, rich in diluent A is the raffinate, while phase E, rich in solvent S, constitutes the extract.

In general, the concentration of solute B in the raffinate is designated by x and in the extract by y. It is then possible to draw the distribution curve or equilibrium curve which represents y in terms of x.

### Rotating discs column (RDC)

In a rotating discs column (RDC-column) the central shaft equipped with fixed discs is rotating. In addition to that annular rings, so called stators are placed on the inside of the column always in the middle of the distance between two discs. These stators can either be made of metal and inserted into the column or can be integrated in column made of borosilicate glass. The discs have a smaller diameter than inner diameter of the stators so that the shaft can be easily dismantled. Diameters and distances have to be adapted to the process. During operation only the rotating speed can be altered beside the throughput.( https://www.dedietrich.com/en/solutions-and-products/extraction/liquid/liquid-extraction/extraction-columns

Figure 74: RDC column (https://kochmodular.com/liquid-liquid-extraction/extraction-column-types/rdc/)

### Quantities of heavy metals in ashes from different plants

#### Fly ash

Figure 75: heavy metals found in MSWI fly ash (FA) (mg/kg)

#### Bottom ash

Figure 76: Heavy metals found in MSWI bottom ash (BA) (mg/kg).

### Extractants (light phase )

Many heavy metlas are essentil trac elements for humans,animals and plamt in small amounts.

In larger amounts cause acute and chronic toxicity. There are Linked to learning disabilities,cancers and even death .Some of this metals are :As, Cd, Cr, Hg, Ni,  Pb, Zn, Cu. At low pH, i.e. below 3 there is high release of Cu, Mn, Zn, Al, Fe but as the pH is increased the major metals Al, Fe and Si are usually less soluble.

| Metals | Extractants |
| --- | --- |
| As | Phosphoric Acid (cyanex273) |
| Cd | Chloride solution - cyanex273 |
| Cr | nitrilotriacetic acid (NTA)- Sulfuric acid, Hydrochloric acid, Nitric acid were at 500⁰C and the range of extraction is from 263 to 222 mg/L. All of them were of industrial grades. |
| Ni | Versatic acid - cyanex 923 and cyanex 272 (Bis(2,4,4-trimethylpentyl)phosphinic acid) |
| Pb | Chloride solution- Cyanex 272(Bis(2,4,4-trimethylpentyl)phosphinic acid) |
| Zn (Nitric acid 0.6-3M)/ pH= 4 | Phosphonic acid (cyanex273 is the best ) – tri octyl phosphine oxide (cyanex 921) and Tributyl phosphate (TBP) dissolved in kerosene. - EDTA |
| Cu | - LIX® 984N (mixture of 2-hydroxy-5-nonylacetophenone oxime and 5-nonylsalicylaldoxime in a high flash diluent), - Acorga® M5640, - LIX® 622N ) – - Cupromex-3302 the maximum net transfer of copper will be about 10g/l,ph=1.2. - ethylendiaminetetraacetate (EDTA), or diethylenetriaminepentaacetate (DTPA) with concentration 3.0% at the pH range 3-9. |
| Hg (liquid at ordinary temperature ) | - Chloroform (OAP,Ph=9.5 ) - By Cyanex 301 (Bis(2,4,4-trimethylpentyl)dithiophosphinic acid) and cyanex 302(Bis(2,4,4-trimethylpentyl)thiophosphinic acid) from hydrochloric acid media |

#### Leaching tests

The prewashed sample was vacuum dried at 75°C over-night and subjected to acid leaching tests. Typically,1.00 g of the prewashed sample of ﬂy ash was mixed with different weights of solid citric acid in 50 ml deionized water while the pH was kept constant at a selected value by adjusting with concentrated HNO₃ or NaOH solution.The effect of citric acid concentration was examined in the concentration range from 0.01 to 0.40 M (=mol/L),and the effect of liquid/solid ratio was examined at 10:1,20:1, and 50:1 (ml:g). After stirring for 1 h, the suspension was ﬁltered and the clear solution was sent for heavy metal content analysis by means of ICP/AES. The leaching time was varied from 5 to 250 min, and the temperature was also varied from 25°C to 60°C for examination of the temperature effect. Nitric acid, sulfuric acid, hydrochloric acid, DL-malic acid, oxalic acid, and acetic acid were also examined to compare their leaching performance.

##### Experimental conditions of leaching (preliminary and main )

Figure 77: Experimental conditions of preliminary leaching tests.

Figure 78: Experimental conditions of main leaching test

Note :6 M = 6mol/L

### Fly ash

A portion of the ﬂy ash was prewashed with distilled water.A 10-g sample of dried ﬂy ash as-received was mixed together with distilled water at varying liquid/solid ratios[5–50:1 (ml:g)] in a beaker and stirred at room temperature of around 25°C. The suspension was sampled at different time intervals up to 16 h. After vacuum ﬁltration, the metallic elements in the leachate were analyzed by using the ICP/AES spectrometre.

### Recovery of Copper (Cu)

Copper is widely used because it has several essential properties for different technological applications, such as applications in electrical materials and construction, transportation and industrial machinery parts, petroleum refining and brass manufacture.

In view of the industrial and economic importance of this metal, there is a great need to separate and recover copper ions using cost effective commercial extractants. Literature review indicates that hydroxyoximes are now used widely as extractants for copper . The extraction of copper from aqueous sulfate solution with new extractant Cupromex-3302 (active substance is the 5-nonylsalicylaldoxime) using a rotating disc contactor (RDC) was investigated. It was observed from batch experiments that the best results were obtained with the initial aqueous pH and concentration of Cupromex-3302 of 1.9 and 10% (v/v) respectively.

Figure 79:process of separation of copper

The maximum extraction efficiency was equal to 87.44% when the values of rotor speed, Qc and Qd were 375 rpm, 1.83 × 10−⁶ m³/ s and 2.33 × 10−⁶ m³ /s respectively. With

- Qc: continuous phase flow rate,

- Qd:dispersed phase flow rate.

Figure 80: Flow sheet of the proposed recovery method developed for Cu from fly ash

### Recovery of zinc

Nitric acid 0.6-3M was used for the ash leaching. The solvent extraction of Zn(II) from acid leachates was carried out using three extraction ligands that have been reported in the literature to be effective in separation of Zn from other metal ions in acid solutions. The ligands used were di- (2,4,4- tri methylpentyl) phosphinic acid (CYANEX 272), tri octyl phosphine oxide (CYANEX 921) and Tributyl phosphate (TBP) dissolved in kerosene and the extractions were carried out at initial pH 2, 3, 4 and 5. A special problem in these extractions is the separation between Zn(II) and Fe(III) from ash leachates. Leaching at pH 4 gives the lowest levels of iron in the leachate and may thus be a good starting point for the solvent extraction step since all tested ligands bind Fe(III) as well as Zn(II). CYANEX 272 gave the best results extracting about 90% of the Zn(II) in the ash leachates to the organic phase. For the fly ash leachate a ligand concentration of 30 vol% in kerosene was needed and for the bottom ash leachate the corresponding concentration was 20 vol%. The other two ligands gave significantly lower extraction results. Literature data indicate that their performance can be much better in a chloride rich media. Thus, they can be interesting to test if ash is leached with hydro chloric acid instead of nitric acid. Based on the results CYANEX 272 is indicated as a suitable extractant for the recovery of zinc from MSWI plant ashes.

Figure 81:process flow chart

### Zinc and copper recovery by  Cyanex 272

Figure 82: . Mass flowscheme of the leaching-extraction process

### Efficiency of leaching

Figure 83: Concentration of metals at each stage: after leaching, in the raffinates after copper and zinc extraction, as well as in the stripping products. nd = not detected.

Figure 84: Percentage Extraction of Zn and Fe with 30 vol % Cyanex 272 from bottom ash leachates

Figure 85: : Percentage extraction of Zn and Fe with 20 vol % Cyanex 272 from bottom ash leachates

Figure 86: Percentage extraction of Zn and Fe with Cyanex 921 from fly ash leachates

## Contribution

### Flow rate of ashes

The  the percentage of the  residues of  incineration   change from 20 to 30 %.Then,to calculate the mass of nitric acid that will be used in leaching the ashes ,we should  determine the flow rate  of ashes.the total mass of residues   is  338kg after incineration of 800 kg of waste during 1 hour .

| Metals | Quantity in ash(mg/kg ) |
| --- | --- |
| Cu | 2678 |
| Zn | 7378 |
| Pb | 7760 |
| Ni | 1906 |
| Cd | 56.6 |
| Cr | 1512 |
| As | 253.35 |
| Hg | 6.67 |

The ash was extracted at a liquid-to-solid ratio (L⁄S)=5 correspond to  5L of nitric acid to leach 1 kg of ash .

### Nitric acid for leaching

As we mentionned that the nitric acid is a suitable acid for our case .It is important to be concentrated ( 15.8 mol/L-1.42 g⁄cm³ ) to avoid the leaching of Fe that will be extracted mechanically . Metals such as nickel Ni, cobalt Co, copper Cu, mercury Hg, zinc Zn  and cadmium Cd dissolve in nitric acid..See below some physical and chemical properties of HNO₃ - H₂O at  20 °C & 1,013 bar :

| Gew % HNO3 | 0 | 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| volumetric mass (g/cm³) | 1,00 | 1,05 | 1,12 | 1,18 | 1,25 | 1,31 | 1,37 | 1,42 | 1,46 | 1,48 | 1,513 |
| Viscosity (mPa·s) | 1,00 | 1,04 | 1,14 | 1,32 | 1,55 | 1,82 | 2,02 | 2,02 | 1,84 | 1,47 | 0,88 |
| Tfus (°C) | 0 | –7 | –17 | –36 | –30 | –20 | –22 | –41 | –39 | –60 | –42 |
| Téb (°C) | 100,0 | 101,2 | 103,4 | 107,0 | 112,0 | 116,4 | 120,4 | 121,6 | 116,6 | 102,0 | 86,0 |
| p(HNO3) (mbar) | 0,0 | 0,0 | 0,0 | 0,0 | 0,0 | 0,3 | 1,2 | 3,9 | 14,0 | 36,0 | 60,0 |
| p(H2O) (mbar) | 23,3 | 22,6 | 20,2 | 17,6 | 14,4 | 10,5 | 6,5 | 3,5 | 1,2 | 0,3 | 0,0 |
| Molarity (mol/l) | 0 | 1,7 | 3,6 | 5,6 | 7,9 | 10,4 | 13,0 | 15,8 | 18,5 | 21 | 24,01 |

Considerring that each hour 800 kg of waste will be incinerate which  forms  338 kg of ashes (bottom ash and fly ash ), this quantity needs :

- Each hour, 1690 L of acid,

- During 10 hours  of incineration , the quantity of ash becomes: 338*10=3380 kg,

- In 10 hour, the amount of acid that we need is 16900 L.

### Preparation of solution

Eash 1 kg of ash needs 5 L of nitric acid .In the mixer then 338 kg grinded  of waste is added to 1690 L of acid of 15.8 mol/l of concentration .

The input of  the column 1 is 70.432 l of this mixture leached .

| metals | g/kg of ash | 338 kg of ashes | metals in 338 of ash(g) | Percentage of metals in 70 L of mixed =4.414, the amount of metals(g) | NOUNS OF extractants | The amount of extractant (ml) |
| --- | --- | --- | --- | --- | --- | --- |
| Cu | 2.678 | 338 | 905.164 | 37.4737896 | LIX® 984N (mixture of 2-hydroxy-5-nonylacetophenone oxime and 5-nonylsalicylaldoxime in a high flash diluent), | 74.9475792 |
| Zn | 7.3 | 338 | 2467.4 | 102.15036 | Cyanex273( Phosphonic acid ) | 204.30072 |
| Pb | 7.76 | 338 | 2622.88 | 108.587232 | Cyanex 272(Bis(2,4,4-trimethylpentyl)phosphinic acid) | 217.174464 |
| Ni | 1.9 | 338 | 642.2 | 26.58708 | Cyanex 272(Bis(2,4,4-trimethylpentyl)phosphinic acid) | 53.17416 |
| Cd | 0.056 | 338 | 18.928 | 0.7836192 | Cyanex273( Phosphonic acid ) | 1.5672384 |
| Cr | 1.51 | 338 | 510.38 | 21.129732 | nitrilotriacetic acid (NTA)- | 42.259464 |
| As | 0.253 | 338 | 85.514 | 3.5402796 | Cyanex273( Phosphonic acid ) | 7.0805592 |
| Hg | 0.00676 | 338 | 2.28488 | 0.094594032 | By Cyanex 301 (Bis(2,4,4-trimethylpentyl)dithiophosphinic acid) and cyanex 302(Bis(2,4,4-trimethylpentyl)thiophosphinic acid | 0.189188064 |

### Freecad design

| amount of extractant (ml) | extractant | metals |
| --- | --- | --- |
| 74.9475792 | LIX® 984N (mixture of 2-hydroxy-5-nonylacetophenone oxime and 5-nonylsalicylaldoxime in a high flash diluent), | Cu |
| 204.30072 | Cyanex273( Phosphonic acid ) | Zn |
| 217.174464 | Cyanex 272(Bis(2,4,4-trimethylpentyl)phosphinic acid) | pb |
| 53.17416 | Cyanex 272 (Bis(2,4,4-trimethylpentyl)phosphinic acid) | Ni |
| 1.5672384 | Cyanex273( Phosphonic acid ) | Cd |
| 42.259464 | nitrilotriacetic acid (NTA)- | Cr |
| 7.0805592 | Cyanex273( Phosphonic acid ) | As |
| 0.189188064 | By Cyanex 301 (Bis(2,4,4-trimethylpentyl)dithiophosphinic acid) and cyanex 302(Bis(2,4,4-trimethylpentyl)thiophosphinic acid) | Hg |

### Operating the Column

- Open the pump and reach the column with 44 l of ash mixed with nitric acid

- When the liquid level in the column reaches the top right nozzle (turn the feed flowrate down to the desired set point.

- Turn on and set the extractant  flowrate to the desired set point by adjusting the pump speed.

- Close the extrait out rotameter when the liquid level reaches the top left (extrait out) nozzle.

- Allow the interface to form between the top mesh and the top left nozzle (extrait out).  The interface appears as an immiscible layer between acid   and extractant with droplets

- Once the interface is formed in the desired location, open the extrait out rotameter slowly until there are flowrates out of the column.

- Adjusting this rotameter is used to control the interface level. Opening the rotameter causes the interface to rise, while closing it causes the interface to drop.

- The optimum setting of this rotameter will allow for a semi-stable interface and give a minimal amount of drift in the interface level.

- Small adjustments should be made in order to keep the interface constant.

- Set the stirrer speed to a setting of 5 using the dial on the top right of the lab equipment panel. Make sure the motor is powered with the top center switch on the right power panel.

- Allow the column to run until steady state is achieved (about hour).

To feed the column in our case with extractant,we need 9890 cm³ (9.89 Liter extractant per batch load). Wotking time about 1 hour.

#### Shutdown Procedure

  - Once the experiments are complete, turn off the agitator and main power switch.

  - Close the feed and solvent ball valves, leaving the raffinate and extract ball valves open.

#### Stripping

The liquid rich in metals sorted  from the sovent extraction column  should be the input to the stripping tank where it is mixed with acid in ordr to wash the metals formed  in the column . After each column ,a tank of stripping is implemented .

# Zinc recycling

## Fly Ash Handling

- Pre-Washing:

- Take a 10 grams sample of dried fly ash

- Mix the sample with distilled water for 5-10mins under the following conditions ( solid/liquid ratio 10:1 (ml/g), number of washing twice) - Under these conditions, the prewash can remove 86% Na, 70% K, 12% Ca, 1.2% Al, and 0.5% Pb from the fly ash.

- Perform vacuum filtration.

- Analyze the metallic elements in the leachate using ICP/AES spectrometer.

- Leaching Tests:

  - Vacuum dry the pre-washed sample at 75ºC overnight

  - Mix 1 gram of the prewashed sample with 40mL (0.1M) citric acid, for a contact time of 20mins, at pH=3 (adjust the pH using concentrated HNO3 and NaOH) and at room temperature.

  - Filter the suspension and send the clear solution for heavy metal content analysis by means of ICP/AES spectrometer.

Optimum metal removal was achieved under the following conditions: liquid/solid ratio 40 (ml:g), citric acid concentration 0.1 M, contact time 20 min, and pH 3.0 at room temperature.

- Required tests: XRD for fly ash powder sample as received and the fly ash residues after water washing and acid leaching

## Bottom Ash Handling (200-250 kg/t)

- Collect fresh bottom ash samples from the burning incinerators and dry them at 25°C.

- Manually separate the un-burnt parts such as the screw, wire, plastics.

- Prior to leaching, reduce the size of the samples to 500microns with a roll crusher in order to remove the magnetic content (Iron Removal).

- Subject the bottom ash samples (Tailings and concentrates) to leaching tests (24hours) in order to notice the amenability of the samples for metal recovery along with optimization of parameters.

- To calculate the mass of nitric acid to use in leaching the ashes, we should determine the flow rate of ashes.

- In example, liquid to solid (L/S) ratio = 5:1  for every 1kg of ashes, add 5L of Nitric acid.

- It is important to be concentrated (15.8 mol/L-1.42 g⁄cm³) to avoid the leaching of Fe that will be extracted mechanically.

- Considering that each hour 800 kg of waste will be incinerated, which forms 338 kg of ashes (bottom ash and fly ash), this quantity needs:

Each hour, 1690 L of acid

During 10 hours of incineration, the quantity of ash becomes 338*10=3380 kg

In 10 hour, the amount of acid that we need is 16900 L

- Liquid-Liquid Extraction Column:

- Add the nitric acid solution (including heavy metals) to the column from the upper left vessel, and keep adding until the nitric acid reaches the level of this vessel.

- Add phosphonic acid from the lower left vessel (3mL phosphonic acid/1L of nitric acid solution)

- Turn on the mixer for a certain time (ex: 1hr), stop a while to see if two separate phases appear.

- If yes, remove the upper layer through the upper right vessel and then remove the lower layer through the lower right vessel.

# Heavy Metals Recycling Test Rig

## Mechanical integration

|  |  |  | parts needed : -4 valve - 4 pipes (4m each) - 3 medium sized tanks - 2 electrical pumps (>1hp) - 4 moukhalef + wasel zira3e - 9 turnes 90 ppr - 2 tees ppr initial cost : ~ 200 $ |
| --- | --- | --- | --- |

## Concept for automation

### Task for Trainees July 2020

### Concept

Requirements:

3 valves

Motor

Geer

2 Flow sensors

3 Check valve

### Automation Algorithm

needed for automation: only 2 solonoid valves (for exits)

algorithm

Open the pump and reach the column with 44 L of ash mixed with nitric acid

When the liquid level in the column reaches the top right nozzle (turn the feed flowrate down to the desired set point

Turn on and set the extractant flowrate to the desired set point by adjusting the pump speed

Close the extrait out rotameter when the liquid level reaches the top left (extrait out) nozzle.

Allow the interface to form between the top mesh and the top left nozzle (extrait out). The interface appears as an immiscible layer between acid and extractant with droplets.

Once the interface is formed in the desired location, open the extrait out rotameter slowly until there are flowrates out of the column.

Adjusting this rotameter is used to control the interface level. Opening the rotameter causes the interface to rise, while closing it causes the interface to drop.

The optimum setting of this rotameter will allow for a semi-stable interface and give a minimal amount of drift in the interface level.

Small adjustments should be made in order to keep the interface constant.

Set the stirrer speed to a setting of 5 using the dial on the top right of the lab equipment panel. Make sure the motor is powered with the top center switch on the right power panel.

Allow the column to run until steady state is achieved (about hour).

Maysaa Kamareddine, Concept for Ashes Recycling Unit, May 2018

Murdoch Mackenzie, Henkel Australia Pty ltd , THE SOLVENT EXTRACTION OF SOME MAJOR METALS - AN OVERVIEW (thesolve.pdf) (about 1998)

REFERENCES

(1) R.B. Sudderth and G.A. Kordosky, “Some Practical Considerations in the

Evalaution and Selection of Solvent Extraction Reagents” Chemical Reagents in

the Mineral Processing Industry. Ed. Malhotra and Riggs. SME 1987

(2) J.M.W. Mackenzie, “Uranium Solvent Extraction Using Tertiary Amines” ALTA

1997 Uranium Ore to Yellow Cake Seminar. ALTA Metallurgical Services,

Melbourne Australia.

(3) K. Soldenhoff, N. Hayward and D. Wilkins, “Direct Solvent Extraction of Cobalt

and Nickel from Laterite Acid-Pressure Leach Liquors” EPD Congress 1998. Ed.

B.Mishra ( The Minerals, Metals and Materials Society, AIME) 1998 p153-165

(4) G.M. Ritcey, “Commercial Processes for Nickel and Cobalt” In Handbook of

Solvent Extraction. Ed Lo, Baird, and Hansen. John Wiley and Sons 1983. P

673

(5) J.M.W. Mackenzie and M.J.Virnig, “Recovery of Nickel from Ammoniacal

Solutions Using LIX® 84-I” Proceedings of ALTA Nickel /Cobalt Pressure

Leaching and Hydrometallurgy Forum, May 1996. Perth West Australia. ALTA

Metallurgical Services Melbourne.

(6) J.M.W. Mackenzie and M.J.Virnig, “Extraction of Nickel from Ammoniacal

Leach Solutions: Extractant and Solution Chemistry Issues” Proceedings of

ALTA 1998 Nickel/Cobalt Pressure Leaching and Hydrometallurgy Forum. May

1998. Perth West Australia. ALTA Metallurgical Services Melbourne

(7) M.J.Price and J.G.Reid, “Separation and Recovery of Nickel and Cobalt in

Ammoniacal Systems: Process Development” Proceedings ISEC 93 , SCI

London 1993 p159.

(8) M.J.Virnig, J.M.W.Mackenzie, and C.Adamson. “ The Use of Guanidine – Based

Reagents for the Recovery of Gold” Hidden Wealth. South African Institute of

Mining and Metallurgy. 1996 p151

(9) R.L.Movsowitz, R.Kleinberger, and E.M.Buchalter, “Application of Pulsed

Colums for Uranium SX From Pilot to Industrial Columns” ALTA 1997 Uranium

Ore to Yellowcake Seminar. ALTA Metallurgical Services, Melbourne 1997

(10) T.A.Post, M.A.Giralico, M.C.Greaves, and G.M.Frazer, “Operational Results

from Optimised Lightnin SX Pumper and Auxilliary Mixer Designs” ALTA 1996

Copper Hydrometallurgy Forum. Brisbane 1996. ALTA Metallurgical Services

Melbourne.

(11) B.Nyman, R.Kuusisto, P.Taipale and J. Lyyra, “Emphaisi on Feed End Settling

in Outokumpu’s VSF Mixer-Settler” Ibid.

Pilot-plant comparison of Bateman pulsed. (PDF Download Available). Available from: https://www.researchgate.net/publication/292139827_Pilot-plant_comparison_of_Bateman_pulsed_columns_and_mixer_settlers_for_the_extraction_and_stripping_of_zinc_in_the_di2-ethylhexylphosphoric_acid_system [accessed Apr 27 2018].

Ali Ibrahim, Ali Awad, Walid Naous, Wasim Al Haj